Copyright 2013 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 035416 - HYDRAULIC CEMENT UNDERLAYMENT

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

SUMMARY

Section includes polymer-modified, self-leveling, hydraulic cement underlayment for application below interior floor coverings.

PREINSTALLATION MEETINGS

Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

ACTION SUBMITTALS

Product Data: For each type of product.

LEED Submittals:

"Product Data for Credit IEQ 4.2" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for priming and sealing coatings.

Product Data for Credit IEQ 4.2: For priming and sealing coatings, documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4.2" Subparagraph below applies to LEED for Schools.

Laboratory Test Reports for Credit IEQ 4.2: For priming and sealing coatings, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

QUALITY ASSURANCE

Some manufacturers approve installers; others do not. Revise "Installer Qualifications" Paragraph below to suit products selected.

Installer Qualifications: Installer who is approved by manufacturer for application of underlayment products required for this Project.

FIELD CONDITIONS

Environmental Limitations: Comply with manufacturer's written instructions for substrate temperature, ventilation, ambient temperature and humidity, and other conditions affecting underlayment performance.

Place hydraulic cement underlayments only when ambient temperature and temperature of substrates are between 50 and 80 deg F (10 and 27 deg C).

PRODUCTS

Manufacturers and products listed in SpecAgent and Masterworks Paragraph Builder are neither recommended nor endorsed by the AIA or ARCOM. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

HYDRAULIC CEMENT UNDERLAYMENTS

Minimum thickness indicated in "Hydraulic Cement Underlayment" Paragraph below indicates capability of material, generally over concrete. Required minimum thickness for application depends on substrate and type of floor covering to be applied. Wood substrates, for example, will require greater minimum thickness. In addition, numerous manufacturers make products with differing compressive strengths, cure times, and suitability for use with radiant flooring. Consult manufacturers.

Hydraulic Cement Underlayment: Polymer-modified, self-leveling, hydraulic cement product that can be applied in minimum uniform thickness of 1/4 inch (6 mm) and that can be feathered at edges to match adjacent floor elevations.

<Double click here to find, evaluate, and insert list of manufacturers and products.>

Cement Binder: ASTM C 150/C 150M, portland cement, or hydraulic or blended hydraulic cement as defined by ASTM C 219.

Revise "Compressive Strength" Subparagraph below to suit Project; consult manufacturers. Products are available in a range of strengths; retain one option or insert value in subparagraph.

Compressive Strength: Not less than [4000 psi (27.6 MPa)] [5000 psi (34.5 MPa)] [6000 psi (41.4 MPa)] <Insert value> at 28 days when tested according to ASTM C 109/C 109M.

Retain "Underlayment Additive" Subparagraph below if required. Some manufacturers recommend additives for applications over cutback adhesive or wood and metal substrates.

Underlayment Additive: Resilient-emulsion product of underlayment manufacturer, formulated for use with underlayment when applied to substrate and conditions indicated.

Retain "Aggregate" Paragraph below if addition of aggregate filler is required by manufacturer to achieve thickness indicated. Coordinate aggregate size with depth of underlayment.

Aggregate: Well-graded, washed gravel, 1/8 to 1/4 inch (3 to 6 mm); or coarse sand as recommended by underlayment manufacturer.

Provide aggregate when recommended in writing by underlayment manufacturer for underlayment thickness required.

Water: Potable and at a temperature of not more than 70 deg F (21 deg C).

When applied over wood, some manufacturers recommend reinforcing their products; consult manufacturers. Retain "Reinforcement" Paragraph below if applicable.

Reinforcement: For underlayment applied to wood substrates, provide galvanized metal lath or other corrosion-resistant reinforcement recommended in writing by underlayment manufacturer.

Primer: Product of underlayment manufacturer recommended in writing for substrate, conditions, and application indicated.

Retain "VOC Content" Subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.2.

VOC Content: Provide primer with VOC content of 200 g/L.

Retain "Low-Emitting Primer" Subparagraph below if required for LEED for Schools Credit IEQ 4.2.

Low-Emitting Primer: Primer shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Surface Sealer" Paragraph if required. Confirm compatibility with floor coverings and floor covering adhesives specified in Division 09 Sections.

Surface Sealer: Designed to reduce porosity as recommended by manufacturer for type of floor covering to be applied to underlayment.

EXECUTION

PREPARATION

General: Prepare and clean substrate according to manufacturer's written instructions.

Treat nonmoving substrate cracks according to manufacturer's written instructions to prevent cracks from telegraphing (reflecting) through underlayment.

Fill substrate voids to prevent underlayment from leaking.

If underlayments are installed over adhesive residues, consult manufacturers for recommendations and revise "Concrete Substrates" Paragraph below.

Concrete Substrates: Mechanically remove, according to manufacturer's written instructions, laitance, glaze, efflorescence, curing compounds, form-release agents, dust, dirt, grease, oil, and other contaminants that might impair underlayment bond.

Retain "Moisture Testing" Subparagraph below if required by manufacturer for underlayment placed on hardened concrete slabs.

Moisture Testing: Perform anhydrous calcium chloride test, ASTM F 1869. Proceed with installation only after substrates do not exceed a maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/100 sq. m)] <Insert value> in 24 hours.

Wood Substrates: Mechanically fasten loose boards and panels to eliminate substrate movement and squeaks. Sand to remove coatings that might impair underlayment bond and remove sanding dust.

Retain subparagraph below if applicable.

Install underlayment reinforcement recommended in writing by manufacturer.

Nonporous Substrates: For ceramic tile, quarry tile, and terrazzo substrates, remove waxes, sealants, and other contaminants that might impair underlayment bond, and prepare surfaces according to manufacturer's written instructions.

Adhesion Tests: After substrate preparation, test substrate for adhesion with underlayment according to manufacturer's written instructions.

APPLICATION

Indicate underlayment thicknesses on Drawings or insert requirements in this article.

General: Mix and apply underlayment components according to manufacturer's written instructions.

Close areas to traffic during underlayment application and for time period after application recommended in writing by manufacturer.

Coordinate application of components to provide optimum adhesion to substrate and between coats.

Retain subparagraph below for moving joints in floor. Detail joints on Drawings and revise below to suit Project.

At substrate expansion, isolation, and other moving joints, allow joint of same width to continue through underlayment.

Apply primer over prepared substrate at manufacturer's recommended spreading rate.

Apply underlayment to produce uniform, level surface.

Retain first subparagraph below if addition of aggregate is required for thickness indicated.

Apply a final layer without aggregate to product surface.

Feather edges to match adjacent floor elevations.

Cure underlayment according to manufacturer's written instructions. Prevent contamination during application and curing processes.

Do not install floor coverings over underlayment until after time period recommended in writing by underlayment manufacturer.

Retain first paragraph below if surface sealer is required in this Section.

Apply surface sealer at rate recommended by manufacturer.

Remove and replace underlayment areas that evidence lack of bond with substrate, including areas that emit a "hollow" sound when tapped.

END OF SECTION 035416