Copyright 2013 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 095113 - ACOUSTICAL PANEL CEILINGS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

SUMMARY

Section includes acoustical panels and exposed suspension systems for ceilings.

PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

ACTION SUBMITTALS

Product Data: For each type of product.

Samples: For each exposed product and for each color and texture specified, 6 inches (150 mm) minimum dimension.

          - Samples for Initial Selection: For components with factory-applied color finishes.

          - Samples for Verification: For each component indicated and for each exposed finish required, prepared on Samples of size indicated below.  Products submitted that are

            - Acoustical Panel: Set of 6-inch- (150-mm-) square Samples of each type, color, pattern, and texture.

            - Exposed Suspension-System Members, Moldings, and Trim: Set of 6-inch (150-mm) long Samples of each type, finish, and color.

INFORMATIONAL SUBMITTALS

Product test reports.

Evaluation reports.

Field quality-control reports.

CLOSEOUT SUBMITTALS

Maintenance data.

QUALITY ASSURANCE

Testing Agency Qualifications: Qualified according to NVLAP.

Mockups: Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

Indicate portion of ceiling represented by mockup on Drawings or draw mockup as separate element.

Build mockup of typical ceiling area as shown on Drawings.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Source Limitations:  Obtain each type of acoustical ceiling panel and supporting suspension system through one source from a single manufacturer.

Seismic Standard:  Provide acoustical panel ceilings designed and installed to withstand the effects of earthquake motions according to the following:

Standard for Ceiling Suspension Systems Requiring Seismic Restraint:  Comply with ASTM E 580.

CISCA's Recommendations for Acoustical Ceilings:  Comply with CISCA's "Recommendations for Direct-Hung Acoustical Tile and Lay-in Panel Ceilings--Seismic Zones 0-2."

CISCA's Guidelines for Systems Requiring Seismic Restraint:  Comply with CISCA's "Guidelines for Seismic Restraint of Direct-Hung Suspended Ceiling Assemblies--Seismic Zones 3 & 4."

UBC Standard 25-2, "Metal Suspension Systems for Acoustical Tile and for Lay-in Panel Ceilings."

ASCE 7, "Minimum Design Loads for Buildings and Other Structures":  Section 9, "Earthquake Loads."

DELIVERY, STORAGE, AND HANDLING

Deliver acoustical panels, suspension system components, and accessories to Project site in original, unopened packages and store them in a fully enclosed, conditioned space where they will be protected against damage from moisture, humidity, temperature extremes, direct sunlight, surface contamination, and other causes.

Store materials inside under cover and keep them dry and protected against damage from weather, direct sunlight, surface contamination, corrosion, construction traffic and other causes. Neatly stack acoustical panels and other materials flat to prevent sagging, warping or any deformation.  Materials shall not be stored in direct contact with concrete slabs.

Before installing acoustical panels, permit them to reach room temperature and a stabilized moisture content.  Handle acoustical panels carefully to avoid chipping edges or damaging units in any way.

PROJECT CONDITIONS

Environmental Limitations:  Do not install acoustical panel ceilings until spaces are enclosed and weatherproof, wet work in spaces is complete and dry, work above ceilings is complete, and ambient temperature and humidity conditions are maintained at the levels indicated for Project when occupied for its intended use.

Pressurized Plenums:  Operate ventilation system for not less than 48 hours before beginning acoustical panel ceiling installation.

COORDINATION

Coordinate layout and installation of acoustical panels and suspension system with other construction that penetrates ceilings or is supported by them, including light fixtures, HVAC equipment, fire-suppression system, and partition assemblies.

EXTRA MATERIALS

Furnish extra materials described below that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Acoustical Ceiling Panels:  Full-size panels equal to [10] [5] [2] percent of quantity installed.

Suspension System Components:  Quantity of each exposed component equal to [10] [5] [2] percent of quantity installed.

Hold-Down Clips:  Equal to [10] [5] [2] percent of quantity installed

PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

PERFORMANCE REQUIREMENTS

Retain "Seismic Performance" Paragraph below for projects requiring seismic design. Delete paragraph if performance requirements are indicated on Drawings. Retain option if International Building Code seismic design requirements prevail. Coordinate requirements with structural engineer.

Seismic Performance: Acoustical ceiling shall withstand the effects of earthquake motions determined according to [ASCE/SEI 7] <Insert requirement>.

Surface-Burning Characteristics: Comply with ASTM E 84; testing by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

Retain one option in "Flame-Spread Index" Subparagraph below.

Flame-Spread Index: Comply with ASTM E 1264 for Class A materials.

Smoke-Developed Index:  50 <Insert value> or less.

ACOUSTICAL PANEL CEILINGS, GENERAL

Glass-Fiber-Based Panels: Made with binder containing no urea formaldehyde.

Acoustical Panel Standard: Comply with ASTM E 1264.

Metal Suspension System Standard: Comply with ASTM C 635.

Attachment Devices: Size for five times the design load indicated in ASTM C 635, Table 1, "Direct Hung," unless otherwise indicated. Comply with seismic design requirements.

Available Manufacturers: Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Armstrong World Industries, Inc.

CertainTeed Corporation.

Chicago Metallic Corporation.

USG Corporation.

ACOUSTICAL PANELS <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation. Use same designation for acoustical panels in this article and for suspension system in "Metal Suspension System" Article; together, they make up the ceiling. Use these designations on Drawings to identify each ceiling assembly.

Do not assume that every combination of fire-resistance rating, classification, pattern, color, light reflectance, acoustical rating, edge detail, thickness, and size listed under each product description is available. Before retaining salient characteristics, verify availability with manufacturers.

Basis-of-Design Product:  Subject to compliance with requirements, provide the following product, or a comparable product from the list of available manufacturers:

Manufacturer: <Insert name> [As indicated in the Drawings].

Type: <Insert type> [As indicated in the Drawings].

Product Name: <Insert product name> [As indicated in the Drawings].

Pattern:  <Insert pattern name> [As indicated in the Drawings].

Color: [White] [As selected from manufacturer's full range] [Match Architect's sample] [As indicated by manufacturer's designation] [As indicated on Drawings] [As indicated in a schedule] <Insert color>.

LR: <Insert LR>.

NRC: <Insert NRC>, Type E-400 mounting according to ASTM E 795.

CAC: <Insert CAC>.

AC: <Insert AC>.

Edge/Joint Detail: [Square] [Reveal sized to fit flange of exposed suspension-system members] [Flush reveal sized to fit flange of exposed suspension-system members] [Beveled, kerfed and rabbeted long edges and square, butt-on short edges] <Insert manufacturer's special proprietary edge detail>.

Thickness:  [9/16 inch (15 mm)] [5/8 inch (15 mm)] [3/4 inch (19 mm)] [7/8 inch (22 mm)] [1 inch (25 mm)] [1-1/2 inches (38 mm)] [2 inches (51 mm)] [3 inches (76 mm)] [As indicated on Drawings] [As indicated in a schedule] <Insert dimension>.

Modular Size: [24 by 24 inches (610 by 610 mm)] [24 by 48 inches (610 by 1220 mm)] [600 by 600 mm] [600 by 1200 mm] [As indicated on Drawings] [As indicated in a schedule] <Insert size>.

METAL SUSPENSION SYSTEM, GENERAL

Metal Suspension System Standard: Provide manufacturer's standard direct-hung metal suspension systems of types, structural classifications, and finishes indicated that comply with applicable requirements in ASTM C 635.

Finishes and Colors, General: Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes. Provide manufacturer's standard factory-applied finish for type of system indicated.

High-Humidity Finish: Comply with ASTM C 635 requirements for "Coating Classification for Severe Environment Performance" where high-humidity finishes are indicated.

Attachment Devices: Size for five times the design load indicated in ASTM C 635, Table 1, "Direct Hung," unless otherwise indicated. Comply with seismic design requirements.

Power-Actuated Fasteners in Concrete: Fastener system of type suitable for application indicated, fabricated from corrosion-resistant materials, with clips or other accessory devices for attaching hangers of type indicated, and with capability to sustain, without failure, a load equal to 10 times that imposed by ceiling construction, as determined by testing per ASTM E 1190, conducted by a qualified testing and inspecting agency.

Wire Hangers, Braces, and Ties: Provide wires complying with the following requirements:

Zinc-Coated, Carbon-Steel Wire: ASTM A 641/A 641M, Class 1 zinc coating, soft temper.

Size: Select wire diameter so its stress at 3 times hanger design load (ASTM C 635, Table 1, "Direct Hung") will be less than yield stress of wire, but provide not less than 0.135-inch- diameter wire.

Seismic Stabilizer Bars: Manufacturer's standard perimeter stabilizers designed to accommodate seismic forces.

Seismic Struts: Manufacturer's standard compression struts designed to accommodate seismic forces.

Seismic Clips: Manufacturer's standard seismic clips designed and spaced to secure acoustical panels in-place.

Delete paragraph below if hold-down clips are not needed.

Hold-Down Clips: Where indicated, provide manufacturer's standard hold-down clips spaced 24 inches o.c. on all cross tees.

Delete paragraph below if gasketing is not needed.

Clean-Room Gasket System: Where indicated, provide manufacturer's standard system, including manufacturer's standard gasket and related adhesives, tapes, seals, and retention clips, designed to seal out foreign material from and maintain positive pressure in clean room.

METAL SUSPENSION SYSTEM <Insert drawing designation>

Copy this article and re-edit for each product.

Insert number to complete drawing designation. Use same designation for acoustical panels in this article and for suspension system in "Metal Suspension System" Article; together, they make up the ceiling. Use these designations on Drawings to identify each ceiling assembly.

Do not assume that every combination of fire-resistance rating, classification, pattern, color, light reflectance, acoustical rating, edge detail, thickness, and size listed under each product description is available. Before retaining salient characteristics, verify availability with manufacturers.

Basis-of-Design Product:  Subject to compliance with requirements, provide Armstrong Seismic RX System with BerCZ clips the following product, or a comparable product from the list of available manufacturers:

Manufacturer: [Armstrong World Industries, Inc.] <Insert name> [As indicated in the Drawings].

Type: [Seismic RX System with BerCZ Clips] <Insert type> [As indicated in the Drawings].

Capped, Double-Web, Steel Suspension System: Main and cross runners roll formed from cold-rolled steel sheet; prepainted, electrolytically zinc coated, or hot-dip galvanized according to ASTM A 653/A 653M, not less than G30 (Z90) coating designation; with prefinished 9/16-inch- (15-mm-) wide metal caps on flanges.

Structural Classification:  Heavy-duty system.

End Condition of Cross Runners: [Override (stepped)] [or] [butt-edge] type.

Face Design: [Flat, flush] [Flanges formed with an integral center reveal].

Cap Material: [Steel] [or] [aluminum] cold-rolled sheet.

Coordinate finish in "Cap Finish" Subparagraph below with metal type selected.

Cap Finish: [Painted white] [Painted in color as selected from manufacturer's full range] [Painted to match color indicated by manufacturer's designation] [Painted to match color of acoustical unit] [Plated with metallic finish as selected from manufacturer's full range] [Plated with metallic finish indicated by manufacturer's designation] [Natural finish for aluminum].

Roll-Formed, Sheet-Metal Edge Moldings and Trim: Type and profile indicated or, if not indicated, manufacturer's standard moldings for edges and penetrations that comply with seismic design requirements; formed from sheet metal of same material, finish, and color as that used for exposed flanges of suspension-system runners.

EXECUTION

EXAMINATION

Examine substrates, areas, and conditions, including structural framing to which acoustical panel ceilings attach or abut, with Installer present, for compliance with requirements specified in this and other Sections that affect ceiling installation and anchorage and with requirements for installation tolerances and other conditions affecting performance of acoustical panel ceilings.

Proceed with installation only after unsatisfactory conditions have been corrected.

PREPARATION

Measure each ceiling area and establish layout of acoustical panels to balance border widths at opposite edges of each ceiling.  Avoid using less-than-half-width panels at borders, and comply with layout shown on reflected ceiling plans.

INSTALLATION

Install acoustical panel ceilings to comply with ASTM C 636/C 636M and seismic design requirements indicated, according to manufacturer's written instructions and CISCA's "Ceiling Systems Handbook."

Measure each ceiling area and establish layout of acoustical panels to balance border widths at opposite edges of each ceiling. Avoid using less-than-half-width panels at borders, and comply with layout shown on reflected ceiling plans.

Arrange directionally patterned acoustical panels as indicated on reflected ceiling plans.

Suspend ceiling hangers from building's structural members and as follows:

Install hangers plumb and free from contact with insulation or other objects within ceiling plenum that are not part of supporting structure or of ceiling suspension system.

Splay hangers only where required to miss obstructions; offset resulting horizontal forces by bracing, countersplaying, or other equally effective means.

Splay hangers only where required to miss obstructions; offset resulting horizontal forces by bracing, countersplaying, or other equally effective means.

Where width of ducts and other construction within ceiling plenum produces hanger spacings that interfere with location of hangers at spacings required to support standard suspension system members, install supplemental suspension members and hangers in form of trapezes or equivalent devices.

Secure wire hangers to ceiling suspension members and to supports above with a minimum of three tight turns.  Connect hangers directly either to structures or to inserts, eye screws, or other devices that are secure and appropriate for substrate and that will not deteriorate or otherwise fail due to age, corrosion, or elevated temperatures.

Do not support ceilings directly from permanent metal forms or floor deck.  Fasten hangers to cast-in-place hanger inserts, postinstalled mechanical or adhesive anchors, or power-actuated fasteners that extend through forms into concrete.

When steel framing does not permit installation of hanger wires at spacing required, install carrying channels or other supplemental support for attachment of hanger wires.

Do not attach hangers to steel deck tabs.

Do not attach hangers to steel roof deck.  Attach hangers to structural members.

Space hangers not more than 48 inches o.c. along each member supported directly from hangers, unless otherwise indicated; provide hangers not more than 8 inches from ends of each member.

Size supplemental suspension members and hangers to support ceiling loads within performance limits established by referenced standards and publications.

Install suspension system runners so they are square and securely interlocked with one another.  Remove and replace dented, bent, or kinked members.

Install acoustical panels with undamaged edges and fit accurately into suspension system runners and edge moldings.  Scribe and cut panels at borders and penetrations to provide a neat, precise fit.

Arrange directionally patterned acoustical panels as follows:

As indicated on reflected ceiling plans.

For square-edged panels, install panels with edges fully hidden from view by flanges of suspension system runners and moldings.

For reveal-edged panels on suspension system runners, install panels with bottom of reveal in firm contact with top surface of runner flanges.

For reveal-edged panels on suspension system members with box-shaped flanges, install panels with reveal surfaces in firm contact with suspension system surfaces and panel faces flush with bottom face of runners.

Paint cut edges of panel remaining exposed after installation; match color of exposed panel surfaces using coating recommended in writing for this purpose by acoustical panel manufacturer.

Install hold-down clips in areas indicated, in areas required by authorities having jurisdiction, and for fire-resistance ratings; space as recommended by panel manufacturer's written instructions, unless otherwise indicated.

Install clean-room gasket system in areas indicated, sealing each panel and fixture as recommended by panel manufacturer's written instructions.

Protect lighting fixtures and air ducts to comply with requirements indicated for 
fire-resistance-rated assembly.

CLEANING

Clean exposed surfaces of acoustical panel ceilings, including trim, edge moldings, and 
suspension system members.  Comply with manufacturer's written instructions for cleaning and touchup of minor finish damage.  Remove and replace ceiling components that cannot be successfully cleaned and repaired to permanently eliminate evidence of damage.

END OF SECTION 095113